12-Hydroxy Stearic Acid (12 HSA)

Product description:

A high-performance fatty acid derived from hydrogenated castor oil. Widely used as a thickening agent and rheology modifier in lubricants. Excellent thermal stability and viscosity. (Right now, in our website)

CAS number: 106-14-9

EC number: 203-366-1

HSN number: 29157040

Typical specifications:

| Acid Value (Fresh Sample) | : 175 Min |
| --- | --- |
| Saponification Value | : 175 - 185 |
| Hydroxyl Value (Fresh Sample) | : 155 Min |
| Iodine Value | : 5 Max |
| Color Gardner | : 4 Max |
| Specific Gravity @ 27 °C | : 0.935 - 0.945 |
| Unsaponiﬁable Matter | : 1 % Max |
| Moisture | : 0.10 % Max |
| Melting Point | : 72 degree C |
| Fatty Acid Composition |  |
| 16:0 Palmitic Acid | : 1-4 |
| 18:0 Stearic Acid | : 0-3 |
| 18:1 Oleic Acid & Isomers | : 3-6 |
| 18:2 Linoleic Acid | : 1-5 |
| Ricinoleic Acid | : 85 Min |
| Other |  |

Applications:

12-Hydroxystearic Acid (12-HSA) finds application in a wide range of industries, including:

- Manufacture of multipurpose lithium, calcium, and lithium complex greases.

- Manufacture of acrylic polymers and other specialty polymers.

- Used as an internal lubricant in the processing and molding of plastics.

- Used in aqueous and non-aqueous coating systems for automotive, industrial equipment, appliances, and architectural applications.

- Used as a shrink-resistant treatment for wool and other textile finishing applications.

- Used in coating formulations, including coatings and can-lining systems for the interior of metal food and beverage containers (subject to applicable regulatory approvals).

- Used as an activator and internal lubricant in natural and synthetic rubber compounds.

- Used as a rheology modifier (thixotropic agent) in inks, coatings, and related formulations.

- Used in the manufacture of specialty chemicals such as esters, ethoxylates, sulfates, and other derivatives for applications in plasticizers, textiles, cosmetics, lubricants, and metalworking fluids.

Packaging options:

Supplied in 25 Kgs/50 Kgs bags as per customer requirement

MSDS / TDS download: We will provide this document, download options should be there when customer details provided (Just like enquiry form)