Castor Oil First Special Grade (FSG)

Product description:

Industrial-grade Castor Oil is a renewable vegetable oil derived from castor seeds (Ricinus communis). Known for its high viscosity, excellent lubricity, and unique hydroxyl fatty acid structure. (Right now, in our website) or/and we can add below

Castor Oil FSG is a pale, yellow viscous liquid free from suspended matter and insoluble in water.

CAS number: 8001-79-4

EC number: 232-293-8

HSN number: 15153090

Typical specifications:

| APPEARANCE | PALE YELLOW VISCOUS LIQUID |
| --- | --- |
| VISCOSITY GARDNER AT 25 ºC | U – V |
| MOISTURE, IMPURITIES & VOLATILE MATTER | 0.25 % MAX |
| ACID VALUE | 2.00 MAX |
| HYDROXYL VALUE | 161-169 |
| IODINE VALUE | 82- 90 |
| SAPONIFICATION VALUE | 177-185 |
| UNSAPONIFIABLE MATTER | 1.00 % MAX |
| ACETYL VALUE | 140 MIN |
| FREE FATTY ACID AS OLEIC ACID | 1 % MAX |
| REFRACTIVE INDEX @ 25 ºC | 1.477 - 1.481 |
| RELATIVE DENSITY @ 20 ºC | 0.954 – 0.960 |
| OPTICAL ROTATION | +3.5 - + 6.0 Deg |
| COLOR IN 5 ¼” LỌVIBOND CELL TINTOMETER | 20-Y 2-R MAX |
| GARDNER COLOR @ 25 ºC | 3 MAX |

Applications:

1. Castor Oil FSG Grade (First Special Grade) (Our Product which is available & targeted)

Applications of Castor Oil FSG Grade

Castor Oil FSG Grade is a high-quality industrial grade vegetable oil obtained from castor seeds. It is widely used as a renewable, bio-based raw material in numerous industrial applications and serves as the starting material for most castor oil derivatives.

✓ In the manufacture of polyurethane resins, elastomers and casting compounds

✓ In the manufacture of alkyd resins, coatings, varnishes and printing inks

✓ As a raw material for the production of sebacic acid, 12-Hydroxy Stearic Acid (12-HSA), Hydrogenated Castor Oil (HCO), Undecylenic Acid and other castor oil derivatives

✓ In the manufacture of lubricants, specialty greases and metalworking fluids

✓ In hydraulic fluids for automobiles, trucks and industrial machinery

✓ As an ingredient in petroleum oil-field de-emulsifiers

✓ As a dielectric fluid for electrical capacitors and condensers

✓ As a specialty fluid for sonar transducers

✓ In textile auxiliaries, leather chemicals and rubber processing

✓ In adhesives, sealants and polymer formulations

✓ As a renewable bio-based raw material for specialty chemicals

| Grade | Major Industries |
| --- | --- |
| Castor Oil FSG Grade | Lubricants, Greases, Polyurethane, Coatings, Electrical, Oilfield Chemicals, Textile, Rubber, Polymers |
| Castor Oil USP/IP/BP Grade | Pharmaceutical, Nutraceutical, Veterinary, Healthcare |
| Castor Oil Cosmetic Grade | Personal Care, Skin Care, Hair Care, Soaps, Cosmetics |

2. Castor Oil USP/IP/BP Grade (Pharmaceutical Grade)

(This Product details only for information which is not planned for sell)

Applications of Pharmaceutical Grade Castor Oil

Pharmaceutical Grade Castor Oil is a highly purified vegetable oil manufactured in compliance with pharmacopeial standards such as USP, IP or BP. It is widely used in pharmaceutical and healthcare formulations.

✓ As an excipient in pharmaceutical formulations

✓ As a lubricant for tablet and capsule manufacturing

✓ In oral liquid formulations

✓ In topical ointments and creams

✓ In medicated lotions

✓ As a pharmaceutical solvent and carrier oil

✓ In laxative formulations (where approved)

✓ In soft gelatin capsule formulations

✓ In veterinary pharmaceutical products

✓ As a starting material for pharmaceutical-grade castor oil derivatives

3. Castor Oil Cosmetic Grade

(This Product details only for information which is not planned for sell)

Applications of Cosmetic Grade Castor Oil

Cosmetic Grade Castor Oil is a highly refined natural vegetable oil widely used in personal care and cosmetic formulations because of its excellent emollient, moisturizing and conditioning properties.

✓ In skin care creams and lotions

✓ In facial serums

✓ In lipsticks and lip balms

✓ In hair oils and conditioners

✓ In shampoos

✓ In soaps and cleansing bars

✓ In massage oils

✓ In nail care products

✓ In beard oils

✓ In baby care products

✓ In natural and herbal cosmetic formulations

Packaging options:

200 Kg Net MS Drum: 16.0 MT Loose / Palletized/20' ctr

225 Kg Net MS Drum: 18.0 MT Loose / Palletized/20' ctr

20’ ISO Ctr: 21.5 MT (+/- 5%)

20’ Flexi bag: 21.5 MT (+/-5%)

MSDS / TDS download: We will provide this document, download options should be there when customer details provided (Just like enquiry form)