Hydrogenated Castor Oil (HCO)

Product description:

Produced by hydrogenating castor oil, HCO is a hard, brittle wax with a high melting point and excellent chemical stability. Superior lubricating and thickening properties. (Right now in Website)       or

Hydrogenated Castor Oil is a wax-like compound obtained by controlled hydrogenation of refined Castor Oil. It is a hard, brittle, high melting point product that is practically odorless and tasteless. It is supplied in the form of flakes. The Color of is cream to white.

CAS number: 8001-78-3

EC number: 232-292-2

HSN number: 15162039

Typical specifications:

| Physical Property: - |  |
| --- | --- |
| 1. Molecular Weight | 938 |
| 2. Specific Gravity (25/25 °C) | 1.0 +/- 0.03 |
| 3. Flash Point | 315°C (COC) |
| 4. Fire Point | 335°C (COC) |
| 5. Ash Content | 0.005 % Max |
| Chemical Property: - |  |
| Appearance | Milky White Flakes |
| Acid Value | 3.00 Max. |
| Hydroxyl Value | 155.00 Min. |
| Iodine Value | 3.00 Max. |
| Saponification Value | 175.00 Min. |
| Color "Gardner" | 3.00 Max. |
| Melting Point | 83°c - 89°c |
| GLC Value: - |  |
| 1. Palmitic Acid | 1-1.5% |
| 2. Stearic Acid | 8-11% |
| 3. Oleic Acid | 0.2 – 0.6 % |
| 4. Arachidic | 0.20 % Max |
| 5. 12- Keto Stearic Acid | 2 % Max |
| 6. 12 – Hydroxy Stearic Acid | 84 -87 % |

Applications:

Hydrogenated Castor Oil (HCO) finds a wide range of industrial applications due to its excellent hardness, high melting point, chemical stability, lubricity, water resistance, and compatibility with numerous formulations.

- In the manufacture of multipurpose Lithium, Calcium and high-performance aviation greases.

- In the manufacture of soaps and cosmetics

- As a mould release agent in the processing of plastics and rubber compounds

- As a component of specialty wax blends for pencils, crayons, lipsticks and deodorant sticks

- In the manufacture of hot-melt coatings and sealants requiring excellent water resistance

- As a coating agent for paper and as an anti-foaming agent

- In the manufacture of automotive refinish acrylic coatings

- As a rheology modifier (thixotropic agent) in paints, coatings, inks, adhesives, sealants and other industrial formulations

- In chlorinated rubber, epoxy and vinyl coatings to improve rheological properties

- In the manufacture of spin finish oils for polyamide (nylon) fiber

- As a plasticizer for cellulosic materials

- As a processing aid for colour concentrates (masterbatches)

- As a surface treatment agent

- In the manufacture of hot-melt adhesives used for packaging, bookbinding, footwear, carpet backing and product assembly

- As an anti-tack and slip additive in plastic processing

- In the manufacture of specialty chemicals such as esters, ethoxylates, sulfates and other derivatives for metalworking fluids, plasticizers and textile auxiliaries.

Packaging options:

Supplied in 25 Kgs reinforced paper bags/ Jumbo bags of 500 Kgs/1000 Kgs Or as per customer requirement.

Available in Flakes and Powder Form also.

MSDS / TDS download: We will provide this document, download options should be there when customer details provided (Just like enquiry form)